Copper-Steel Clad Sheet:

*Carbon steel as basic metal, cladded with T2 red copper/brass H65/C22000 /CZ101.can be one side cladding or both sides cladding.

*Special technical treatment to merged the two material into a single whole and can not be pilled off

*Thickness combination can be customerized.

*High strength,good electrical and thermal conductivity ,excellent corrosive resistance and extensibility.

*Applications:electronic spare parts,USB sockets, connectors, automobile radiators, gas heaters, LED spare parts, coins, hardware industries,decoration etc

*Base layer material: Simple carbon steel / Q195

*Clad layer material: Brass H90 / C22000/CZ101

*Thickness range: 0.2mm ~2.0mm

*Width: 25mm~470mm

*Applications: Bullet shell, Game coin, Indoor decorations etc.

Advantages for bullet shell:

*Ensuring the performance of the bullet

*Saving the brass material,low cost

*preventing the corrosion occur when using or storage

*The lubrication of surface brass can reduce the bullet’s wearing to the

Chamber

*Excellent cold pressing manufacturability

Mechanical performance:

| No | Temper | Tensile Strength (N/mn2) | Elongation (%) | Applications |
| --- | --- | --- | --- | --- |
| 1 | TM | ≥280 | ≥45 | Extremely good extensibility, Suitable for very deep pressing |
| 2 | M | ≥290 | ≥33 | Good extensibility, Suitable for general pressing capabilities |
| 3 | Y₂ | 350-450 | ≥5 | With certain degree of extensibility, Suitable for components requiring bending and certain strength |
| 4 | Y | ≥460 | - | Suitable for components processed through flat punching or simple bending with requirements for strength |
| 5 | TY | ≥650 | - | Very high strength, Fatigue resistance, and electricity |

Note: TM temper: Extreme soft, M temper: Soft

Y₂temper: Semi-hard, Y temper: Hard, TY temper: Extra hard